GCA Material Specification:

GCA will conform to the Uniform Guide Specifications (UFGS) 32.11.23 and the equivalent American Association of State Highway Transportation Officials (ASSHTO) #57

GCA consists of clean, sound, durable particles of crashed stone, angular sand, or other such approved materials. Stock must be free of silt and clay as defined by ASTM D247

The maximum Liquid limit and Plasticity index of material passing through N. 40 sieve is 25 and 5 respectively.

Limit the percentage of loss of GCA to a maximum of 40 percent when tested in accordance with ASTM C131/C131

Gradation by percentage must follow the specifications in Table 1:

| Table1: Percentage By Weight Passing Square – Mesh Sieve |  |
| --- | --- |
| 1 inch | 100 |
| ½ inch | 40-70 |
| No. 4 | 20-50 |
| N. 10 | 15-40 |
| No. 40 | 5-25 |
| No. 200 | 0-8 |

Acceptance of GCA is based on compliance with tolerance present in Table 2. Remove any material found to be non-compliance and replace with compliant Material to meet requirements of this specification.

| Table 2: Compliance Tolerances |  |
| --- | --- |
| Grade | Plus, ¼ inch, minus ½ inch |
| Smoothness | Plus/Minus 3/8 inches |
| Individual Test Toal Thickness | Plus/Minus ½ inches |
| Average Job Thickness | Plus/Minus ¼ inches |
| Compaction | Minimum 100% |