# Master SOW for Paint, Paint Thinner and Blasting Media

Blanket Purchase Agreements

# Mississippi River Project Office

# A. General Information

- Description of Purchase: Paint Primer, Blast Media and Paint Thinner Materials.

- Application of the Purchase: To purchase paint material to preserve surfaces of Lock and Dam Tainter Gates.

- Scope Of Work:

- Vinyl zinc-rich (Formula VZ-108d) in 5-gallon ready mix containers. (Formula to follow).

- White Vinyl Paint (Formula V-766e) in 5-gallon ready mix containers. (Formula to follow).

- Gray Vinyl Paint (Formula V-766e) in 5-gallon ready mix containers. (Formula to follow).

- Contractor to submit paint sample(s) to paint lab within 7 calendar days of contract award if not previously tested.

- MEK Paint Thinner ASTM D740 in 5-gallon ready use containers.

- Coal Slag Media Black Diamond 1240 or equivalent. In 4000 lbs. sacks or Bulk 25-ton truck. Heavy-duty applications, providing a moderate profile for near-white blasting.

- Delivery Locations:

Supplies are to be delivered to Mississippi River Project - Service Base, located at 25549 182nd Street, Pleasant Valley, IA  52767 within 12 calendar days after paint lab approval if paint has not already been approved. Delivery personnel must be verified through E-Verify program.

- Technical Point of Contact:

Specified at the call order level.

- Requested by:

US Army Corps of Engineers

Mississippi River Project Office

25549 182nd Street

Pleasant Valley, IA 52767

- Testing (if not previously tested prior to award):

- Paint shall be tested by:

US Army Construction Engineering Research Lab (CERL)

2902 Farber Drive

PO Box 9005

Champaign, IL 61826.

POC: Brooke Divan, phone 217-373-3364

- All tests will be made by and at the expense of the Government; however, expenses for retests because of failure of the first test will be borne by the contractor.

- Inspection will be made at  destination.

- See below for packaging, marking, and testing.

- Pre-certified coatings are acceptable, provided proof of certification documents are submitted to CERL (para. 9.a).  Per-certified documents are valid for up to one year from date of acceptance.

- UPON NOTIFICATION OF INSPECTION RESULTS PLEASE DELIVER TO:

Mississippi River Maintenance Section

25549 182nd Street

Pleasant Valley, IA  52767

- NO FRIDAY OR WEEKEND DELIVERIES PLEASE.

# B. Specifications for Special Formulation Paints and Primers

## GENERAL.

Paints, vehicles, and accessory materials shall have the composition as indicated in the applicable formula or standard specification listed herein.  Paints shall be made only with ingredient materials taken directly from the producers standard packages in those cases where such packaging is normal for the raw material specified and packages shall be unbroken until just prior to incorporation of the contents into the finished product.  Paint and vehicle formulations and miscellaneous materials required under the contract shall be compounded from or conform to materials meeting the requirements of the applicable specifications.  Formulations and procedures as well as raw materials are set forth as follows:

## PAINT PACKAGING, DELIVERY, AND STORAGE.

  - Paints shall be processed and packaged to ensure that within a period of one year from date of manufacture, they will not gel, liver, or thicken deleteriously, form gas in the closed container, or be required to screen lumps. Paints, unless otherwise specified or permitted, shall be packaged in standard Containers not larger than 5 gallons 20 liters, with removable friction or lug-type covers. Containers for vinyl-type paints shall be lined with a coating resistant to solvents in the formulations and capable of effectively isolating the paint from contact with the metal container. Each container of paint or separately packaged component thereof shall be labeled to indicate the purchaser's order number, date of manufacture, manufacturer's batch number, quantity, color, component identification and designated name, and formula or specification number of the paint together with special labeling instructions, when specified. Paint shall be delivered to the job in unbroken containers. Paints that can be harmed by exposure to cold weather shall be stored in ventilated, heated shelters. All paints shall be stored under cover from the elements and in locations free from sparks and flames.

  - Except as otherwise specified or indicated, material shall be packaged for shipping in new non-returnable sheet metal containers of not less than 26 gauge conforming to the applicable requirements of the Interstate Commerce Commission for shipment by railroad, in the specified sizes.  All exterior container surfaces including 5-gallon pail bottoms shall be painted with a pigmented coating.  Containers for solvents and thinners shall be drum type of 5 gallon or 55-gallon size, as specified in the bid schedule, which will require no packing.  One-gallon cans for solvents and thinners shall be of the rectangular type, packed for shipment in accordance with commercial practice.  The 5-gallon containers for pigmented paint shall be of the lug-cover type.  Five-gallon containers for all vinyl type paints shall be lined with a coating resistant to the solvents used in the vinyl formulations, and the lining shall be capable of effectively isolating the vinyl paints from direct contact with the metal container.  LINED CONTAINERS SHALL BE SUBMITTED TO US ARMY CONTRUCTION ENGINEERING RESEARCH LABORATORY (CERL), 2902 FARBER DRIVE, PO BOX 9005, CHAMPAIGN, IL  61826, FOR APPROVAL BEFORE PACKAGE OF THE VINYL TYPE PAINTS.  One-gallon size containers or pigmented paints shall be of the friction-closure type.

  - Fifty-five (55) gallon drums, when specified for solvents and vehicles, shall be the standard closed end type with threaded and capped holes in one end.  Each container shall be clearly and durably labeled and each label shall state that the container is flammable and the use of adequate ventilation and respirators are required.  They should also indicate the contract number; the schedule designation and item number; the date of manufacture; manufacturer’s batch number; quantity; and full name, color, and formula (or specification) designation of the enclosed material as it appears in the schedule, so that it can be quickly and conveniently identified, together with any specified instruction to the user, all as approved by the Contracting Officer.

## MARKING.

The required marking for labels can be found with the appropriate item in Section C, and in paragraph (f) “Labels and Other Forms of Warning”, below.

- Labels and Other Forms of Warning

- The chemical manufacturer, importer, or distributor shall ensure that each container of hazardous chemicals leaving the workplace is labeled, tagged or marked with the following information:

  - Identify of the hazardous chemical(s)

  - Appropriate hazard warnings and

  - Name and address of the chemical manufacturer, importer, or other responsible party.

- Chemical manufacturers, importers, or distributors shall insure that each container of hazardous chemicals leaving the workplace is labeled, tagged, or marked in accordance with this section in a manner which does not conflict with the requirements of the Hazardous Materials Transportation Act (18 U.S.C 1801 e (acq) and regulations issued under that Act by the Department of Transportation.

- If the hazardous chemical is regulated by OSHA in a substance-specific health standard, the chemical manufacturer, importer, distributor, or employer shall ensure that the labels or other forms of warning sued are in accordance with the requirements of that standard.

- Except as provided in paragraphs (f)(5) and (f)(6) the employer shall ensure that each container of hazardous chemicals in the workplace is labeled, tagged or marked with the following information:

  - Identify of the hazardous chemical(s) contained therein, and

  - Appropriate hazard warning

- The employer may use signs, placards, process sheets, batch tickets, operating procedures or other such written materials in lieu of affixing labels to individual stationary process containers as longs as the alternative method identifies the containers to which it is applicable and conveys the information required by paragraph (f)(4) of this section to be on a label.  The written materials shall be readily accessible to the employees in their work area throughout each work shift.

- The employer is not required to label portable containers into which hazardous chemicals are transferred from labeled containers, and which are intended only for the immediate use of the employee who performs the transfer.

- The employer shall not remove or deface existing labels on incoming containers of hazardous chemicals unless the container is immediately marked with the required information.

- The employer shall ensure that labels or other forms of warning are legible in English and prominently displayed on the container, or readily available in the work area throughout each work shift.  Employers having employees who speak other languages may add the information in their language to the material presented, as long as the information is presented in English as well.

- The chemical manufacturer, importer, distributor or employer need not affix new labels to comply with this section if existing labels already convey the required information.

## FORMULATIONS AND PROCEDURES.

Special paint formulas shall comply with the following:

### Formula VZ-108d

This formula is for Vinyl-Type Zinc-Rich Impacted Immersion Coating, the ingredients are shown below.

Table 1 - COMPONENT A

| INGREDIENTS | PERCENT BY WEIGHT | POUNDS | GALLONS |
| --- | --- | --- | --- |
| Vinyl Resin, Type 3 | 16.6 | 109.2 | 9.65 |
| Methyl Isobutyl Ketone | 80.6 | 528.9 | 79.30 |
| Suspending Agent E | 0.7 | 4.6 | 0.28 |
| Suspending Agent F | 0.4 | 2.7 | 0.19 |
| Methanol | 0.5 | 3.3 | 0.50 |
| Synthetic Iron Oxide (Red) | 1.2 | 7.9 | 0.19 |
| Totals | 100.0 | 656.6 | 90.11 |

Table 2 - COMPONENT B

| INGREDIENTS | PERCENT BY WEIGHT | Pounds | Gallons |
| --- | --- | --- | --- |
| Silane B | 100.0 | 4.1 | 0.47 |

Table 3 - COMPONENT C

| INGREDIENTS | PERCENT BY WEIGHT | Pounds | Gallons |
| --- | --- | --- | --- |
| Zinc Dust | 100.0 | 550.0 | 9.42 |
|  | (mixed paint) |  |  |

a.  The iron oxide and suspending agents shall be dispersed into the vehicle (Component A) to a fineness of grind of not less than 4 on the Hegman scale (ASTM D 1210).  Grinding in steel-lined containers or using steel-grinding media shall not be permitted.  The paint shall show the proper proportions of specified materials when analyzed by chromatographic and/or spectrophotometric methods. The sole purpose of the iron oxide pigment is to produce a contrasting color.  A red iron oxide-type 3 vinyl resin vehicle paste may be used in place of dry iron oxide provided compensating adjustment are made in the additions of Type 3 resin and methyl isobutyl ketone.  The finished product with zinc dust added shall produce a paint which has a red tone upon drying and a reflectance of not more than 16 (ASTM E 1347).

b. VZ-108d paint shall be supplied as a kit.  Each kit shall consist of 4.5 gallons ( 33.1 pounds) of Component A in a 5-gallon lug closure type pail,  27.5 pounds of zinc dust (Component C) packaged in a 1-gallon plastic pail, and 3 fluid ounces of silane (Component B) packaged in a glass bottle of suitable size having a polyethylene lined cap.  The bottle of silane shall be placed on the zinc dust in the 1-gallon pail.  In addition to standard labeling requirements, each container of each component shall be properly identified as to component type and each container label of Component A shall carry the following:  MIXING AND APPLICATION INSTRUCTIONS:  WARNING - THIS PAINT WILL NOT ADHERE TO STEEL SURFACES UNLESS COMPONENT B IS ADDED.  Remove the 3 ounces of bottled Component B (silane) from the Component C (zinc dust) container and add to the base paint Component A) with thorough stirring.  Then sift the zinc dust into the base paint while it is being vigorously agitated with a power-driven stirrer and continue the stirring until the zinc dust has been dispersed.  The mixed paint shall at some point be strained through a 30-60 mesh screen to prevent zinc dust slugs from reaching the spray gun nozzle.  The paint shall be stirred continuously during application at a rate that will prevent settling.  If spraying is interrupted for longer than 15 minutes, the entire length of the hose shall be whipped vigorously to redisperse the zinc.  If the spraying is to be interrupted for more than 1 hour, the hose shall be emptied by blowing the paint back into the paint pot.  Thinning will not normally be required when ambient temperatures are below about 80 degrees F, but when the ambient and steel temperatures are higher, methyl isoamyl ketone (MIAK) or methyl isobutyl ketone (MIBK) should be used.  If paint is kept covered at all times, its pot life will be about 8 days.

### Formula V-766e

This formula is for Vinyl-Type White (or Gray) Impacted Immersion Coating, the ingredients are shown below.

| INGREDIENTS | PERCENT BY MASS |
| --- | --- |
| Vinyl Resin, Type 3 | 5.6 |
| Vinyl Resin, Type 4 | 11.6 |
| Titanium Dioxide and (for Gray) Carbon Black | 13.0 |
| Plasticizer | 2.9 |
| Methyl Isobutyl Ketone | 32.0 |
| Toluene | 34.7 |
| Ortho-Phosphoric Acid | 0.2 |
| Total | 100 |

a. The dispersion of pigment shall be accomplished by means of pebble mills or other approved methods to produce a fineness of grind (ASTM D 1210) of not less than 7 on the Hegman scale.  Grinding in steel-lined or steel-ball mills will not be permitted.  No grinding aids, antisettling agents, or any other materials except those shown in the formula will be permitted.  The paint shall show the proper proportions of specified materials when analyzed by chromatographic and/or spectrophotometric methods.  The ortho-phosphoric acid shall be measured accurately and diluted with at least four parts of ketone to one part of acid and it shall be slowly incorporated into the finished paint with constant and thorough agitation.

b. The viscosity of the paint shall be between 60 and 90 seconds using ASTM D 1200 and a No. 4 Ford cup.

c. The white and gray paints shall be furnished in the volume ratio designated by the purchaser.  The gray paint shall contain no pigments other than those specified.  Enough carbon black shall be included to produce a dry paint film having a reflectance of 20-24 (ASTM E 1347).  The resulting gray color shall approximate color 26231 of FED-STD-595.

### Ingredients for Special Paint Formulas.

The following ingredient materials and thinners apply only to the special paints formulas shown above as applicable.

1.  Pigments and Suspending Agents.

- Aluminum Powder For vinyl paint aluminum powder shall conform to ASTM D 962, Type 1, Class B.

- Carbon Black Carbon Black shall conform to ASTM D 561, Type I or II.

- Iron Oxide Iron oxide, (Dry) synthetic (red), shall conform to ASTM D 3721.  In addition, the pigment shall have a maximum oil absorption of 24 and a specific gravity of 4.90 to 5.20 when tested in accordance with ASTM D 281 and ASTM D 153, Method A, respectively.  When the pigment is dispersed into specified vinyl paint formulation, the paint shall have color approximating FED-STD-595 color 10076 (dark red paint), and shall show no evidence of incompatibility or reaction between pigment and other components after 6 months storage.

2.  Titanium Dioxide Titanium dioxide in vinyl paint Formula V-766e shall be one of the following:  Kronos 2160 or 2101, Kronos, Inc.; Ti-Pure 960, E.I. Dupont DeNemours and Co., Inc.

- Resins, Plasticizer, and Catalyst

- Diisodecyl Phthalate Diisodecyl Phthalate shall have a purity of not less than 99.0 percent, shall contain not more than 0.1 percent water, and shall have an acid number (ASTM D 1045) of not more than 0.10.

3.  Vinyl Resin, Type 3

Vinyl resin, Type 3, shall be a vinyl chloride-acetate copolymer of medium average molecular weight produced by a solution polymerization process and shall contain 85 to 88 percent vinyl chloride and 12 to 15 percent vinyl acetate by weight. The resin shall have film-forming properties and shall, in specified formulations, produce results equal to Vinylite resin VYHH, as manufactured by the Union Carbide Corporation.

4.  Vinyl Resin, Type 4

Vinyl resin, Type 4, shall be a copolymer of the vinyl chloride-acetate type produced by a solution polymerization process, shall contain (by weight) 1 percent interpolymerized dibasic acid, 84 to 87 percent vinyl chloride, and 12 to 15 percent vinyl acetate. The resin shall have film-forming properties and shall, in the specified formulations, produce results equal to Vinylite resin VMCH, as manufactured by the Union Carbide Corporation.

5.  Ortho-phosphoric Acid

Ortho-phosphoric acid shall be a chemically pure 85-percent grade.

# C. Specifications for Solvent and Thinners

Methyl Isobutyl Ketone Methyl isobutyl ketone (MIBK) shall conform to ASTM D740

## TESTING

- Chromatographic Analysis Solvents in vinyl paints and thinners shall be subject to analysis by programmed temperature gas chromatographic methods and/or spectrophotometric methods, employing the same techniques that give reproducible results on prepared control samples known to meet the specifications. If the solvent being analyzed is of the type consisting primarily of a single chemical compound or a mixture or two or more such solvents, interpretation of the test results shall take cognizance of the degree of purity of the individual solvents as commercially produced for the paint industry.

- Vinyl Paints Vinyl paints shall be subject to the following adhesion test. When V-766 or V-106 formulations are tested, 5 to 7 mils125 to 175 microns (dry) shall be spray applied to mild steel panels. The steel panels shall be essentially free of oil or other contaminants that may interfere with coating adhesion. The test panels shall be dry blast cleaned to a White Metal grade which shall be in compliance with SSPC SP 5. The surface shall have an angular profile of 2.0 to 2.5 mils50 to 63 microns as measured by ASTM D 4417, Method C. When V-102 or V-103 formulations are tested, they shall be spray applied over 1.5 to 2.5 mils38 to 63 microns (dry) of V-766 or V-106 known to pass this test. When VZ-108 is tested, the coating shall SECTION 09965A Page 39 be mixed in its proper proportions and then spray applied to a dry film thickness of 1.5 to 2.5 mils38 to 63 microns above the blast profile. The VZ-108 shall be top coated with a V-766 known to pass this test. In all cases, the complete system shall have a total dry film thickness of 5 to 7 mils125 to 175 microns above the blast profile. After being air dried for 2 hours at room temperature, the panel shall be dried in a vertical position for 16 hours at 120 degrees F50 degrees C. After cooling for 1 hour, the panel shall be immersed in tap water at 85 to 90 degrees F30 to 32 degrees C for 48 to 72 hours. Immediately upon removal, the panel shall be dried with soft cloth and examined for adhesion as follows: With a pocket knife or other suitable instrument, two parallel cuts at least 1 inch 2.5 centimeters long shall be made 1/4 to 3/8 inch .5 to 1.0 centimeter apart through the paint film to the steel surface. A third cut shall be made perpendicular to and passing through the end of the first two. With the tip of the knife blade, the film shall be loosened from the panel from the third cut between the parallel cuts for a distance of 1/8 to 1/4 inch .3 to .6 centimeter. With the panel being held horizontally, the free end of the paint film shall be grasped between the thumb and forefinger and pulled vertically in an attempt to remove the film as a strip from between the first two cuts. The strip of paint film shall be removed at a rate of approximately 1/10 inch.2 centimeter per second and shall be maintained in a vertical position during the process of removal. The adhesion is acceptable if the strip of paint breaks when pulled or if the strip elongates a minimum of 10 percent during its removal. Paints not intended to be self-priming shall exhibit no delamination from the primer.

## 2.GENERAL

Vinyl paints shall be spray applied, except that areas inaccessible to spraying shall be brushed.  All of the vinyl paints require thinning for spray application except the zinc-rich vinyl paint (Formula VZ 108d) which will normally require thinning only under certain weather conditions.  Thinners for vinyl paints shall be as follows:

APPROXIMATE AMBIENT AIR TEMPERATURE

Degrees Fahrenheit	Degrees Celsius

Below 50 [Below 10]				MEK

50 – 70 [10-21]					MIBK

Above 70 [Above 21]				MIAK

## INSPECTION AND ACCEPTANCE TERMS

- SPECIAL TESTS.

- Boiling water resistance shall be determined in accordance with (ASTM D 1308 Sec.6.4).  Tin panels prepared in accordance with Method No. 2012 shall be dipped in the material to be tested, drained, and allowed to dry 72 hours prior to immersion.  Immersion shall be distilled water at 100 degrees C. (212 degrees F.) for the specified number of hours.  The panels during immersion shall be in the vertical position.  A recovery period of 2 hours shall be allowed before examination of the panel under test.  Acceptable specimens shall show no whitening, dulling, or blistering.

- Alkali Resistance.  Dip the closed end of well-cleaned 1 by 6-inch test tube to a depth of 4 inches into the coating to be tested, and allow to dry for 72 hours in an inverted position—that is, with the mouth of the test tube down.  Place the end of the test tube that was uppermost during the drying period 2 inches below the surface of a 5 percent caustic soda (NaOH) solution at 20 degrees C.  (68 degrees F.) for the specified period of time.  After removal immediately rinse under gently running tap water, holding near the mouth of the tube and being careful not to touch the treated film.  Dry for 2 hours and examine under suitable light.  Acceptable specimens shall show not visible dulling, checking, or blistering.  Defects at the extreme bottom of the test tube shall be disregarded.

- Reactivity of Vehicle shall be determined in accordance with ASTM D 154, “Testing Varnishes”.

- Volatiles in vinyl and epoxy paints and separate thinners therefore are subject to analysis of gas chromatrographic methods.  Upon analysis, the results shall agree with those obtained on a control sample of material that is known to be of the correct composition.  Presence of ingredients other than in the proportions specified or the presence of non-specified ingredients will forma basis for rejecting the material.

- Adhesion Test.  All vinyl paints are subject to the following adhesion test.  When V-766 or V-106 formulations are tested, 5-7 mils (dry) shall be spray applied over to mild steel panels sandblasted to white metal.  When V-102 or V-103 formulations are tested, they shall be spry applied over 1.5 to 2.5 mils (dry) of V-766e known to pass this test.  In all cases, the complete system shall have a total dry film thickness of 5-7 mils above the sandblast profile.  After being air dried for 2 hours at room temperature, the panel shall be dried in a vertical position for 16 hours at 120 degrees F.  After cooling for one (1) hour, the panel shall be immersed in tap water at 85-95 degrees F.  for 48-72 hours.  Immediately upon removal, the panel shall be dried with a soft cloth and examined for adhesion as follows:  With a picket knife or other suitable instrument, two parallel cuts at least 1” long shall be made ¼” to 3/8” apart through the paint film to the steel surface.  A third cut shall be perpendicular to and passing through the ends of the first two.  With the tip of the knife blade, the film shall be loosened from the panel from the third cut between the parallel cuts for a distance of 1/8” to ¼”.  With the panel being held horizontally, the free end of the paint film shall be grasped between the thumb and forefinger and pulled vertically so as to remove the film as a strip from between the first two cuts.   The strip of the paint film shall be removed at a rate of approximately 1/10’ per second, and shall be maintained in a vertical position during the process of removal.  Upon being removed by this method, the paint film shall either break or elongate a minimum of 10%.  Paints not intended to be self-priming shall exhibit no delamination from the primer.

- INSPECTION AND SAMPLES

- The Contracting Officer, or his duty authorized representative, shall have the right to inspect the manufacturing of vehicles and mixed paints, and the packaging, labeling, and shipment of all finished products.  He will collect samples of each batch of each item being furnished, including separate samples of each batch of each phenolic varnish employed as a vehicle component in a pigmented paint, unless the varnishes have been previously tested and approved by the Contracting Officer prior to compounding into the finish paint product.  The inspector will witness the placing, sealing, and labeling of the finished product.  The inspector will witness the placing, sealing, and labeling of the finished products in containers for shipment.  After the samples of the finished products have been tested and approved, shipment is authorized.  Finished materials more than six months old will require retesting.   The presence of the inspector in the plant will not relieve the Contractor from the responsibility for furnishing products fully meeting the specification requirements.  The Contracting Officer reserves the right to test delivered paint for conformance with specification requirements after delivery and prior to the time of making payment therefore.

- Samples of mixed paints, vehicles, drying oils and thinners shall be one-quart size.  Samples of pigments and solid resins shall be approximately one pound in quantity.  Samples of miscellaneous raw materials shall be of appropriate quantity.  All samples shall be submitted to:

U.S. Army Construction Engineer Research Laboratory, (CERL), Corps of Engineers

ATTN:  Rebecca Wilson

2902 Farber Dr.,

PO BOX 9005

Interstate Research Park

Champaign, IL  61280

Unless otherwise authorized, all first tests will be made by and at the expense of the Government.  Any retesting of the samples because of failure of the first tests will be made by the same laboratory, HOWEVER, THE EXPENSE WILL BE BORNE BY THE CONTRACTOR.  A check made payable to “Treasurer of the United States” in the amount of $775.00 for EACH retesting of paint and $775.00 for EACH retesting of thinner will be sent with each sample submitted for retest to CERL.

NOTE:  The following label shall be placed on all containers:

WARNING:  The contents may become acidic over a period of time.  Retesting is recommended if not used within one year after date manufactured.

# D. Blasting Media (Coal Slag Media)

This supply item does not need a specifications section. Paragraph 3.e provides the information needed for vendors to supply this.